TCM207

产品简介 General Information

- TCM207是一款适用于阳离子固化的双官能团氧杂环丁烷单体。它能提高体系固化速度，降低收缩率。由于其独特的三元环氧与四元环氧并存结构，TCM207粘度极低，稀释性极佳。

- TCM207 is a bifunctional oxetane suitable for cationic curing. It can improve curing speed, reduce the shrinkage. Due to its unique structure which has both ternary and quaternary epoxy, TCM207 has very low viscosity and great dilution.

产品信息 Product Information

- 化学名称 Chemical Name：3-乙基-3-[(氧化乙烯-2-甲氧基)甲基]氧杂环丁烷 (3-Ethyl-3-((oxiran-2-ylmethoxy) methyl) oxetane

- 分子量 Molecular Weight：172.22

- CAS No：15957-34-3

技术参数 Technical Parameters

- 外观 Appearance：无色透明液体 Colorless transparent liquid

- 纯度 Purity (GC)：≥97.00

- 水分 Water Content：≤0.30%

产品优势 Benefits

- 高反应活性 High reactivity

- 极低的粘度 Very low viscosity

应用 Applications

- TCM207最常作为单体用于喷墨，也可以用于稀释其他氧杂环丁烷、树脂、单体。

- TCM207 is mostly used as a monomer for inkjet, and can also be used to dilute other oxetanes, resins and monomers.

存储及包装 Storage & Packaging

- 保存在密闭容器中储存在阴凉、干燥、阴暗、通风的区域。自生产日期开始，1年内有效。包装：200kg/桶。

- Keep in a tightly closed container and store in a cool, dry, dark, ventilated area. Effective from the date of production, within 1 year. Packaging: 200kg/drum.

THE END