THM202

产品简介 General Information

- THM202是一款同时适用于自由基和阳离子体系的双官能团氧杂环丁烷单体。它能平衡不同的固化体系，形成网状聚合结构，以此获得更佳的固化效果。

- THM202 is a bifunctional oxetane suitable for both free radical and cationic curing. It can form a network polymerization structure with the balance of different curing systems, so as to obtain better curing performance.

产品信息 Product Information

- 化学名称 Chemical Name：3-乙基-3-甲氧基氧杂环丁烷甲基丙烯酸酯 3-Ethyl-3-(methacryloyloxy)methyl oxetane

- 分子量 Molecular Weight：184.00

- CAS No：37674-57-0

技术参数 Technical Parameters

- 外观 Appearance：浅黄色至无色透明液体 Light yellow to colorless transparent liquid

- 纯度 Purity (GC)：≥97.00%

- 粘度 Viscosity (25ºC)：1~10cps

产品优势 Benefits

- 高反应活性 High reactivity

- 自由基和阳离子均可用 Suitable for both free radical and cationic curing

应用 Applications

- THM202可用于自由基-阳离子混杂体系，常作为单体用于电子材料封装和特种胶粘剂。

- THM202 can be used in radical-cationic systems. It’s often used as a monomer for electronic material packaging and special adhesives.

存储及包装 Storage & Packaging

- 保存在密闭容器中储存在阴凉、干燥、阴暗、通风的区域。自生产日期开始，6个月内有效。包装：200kg/桶。

- Keep in a tightly closed container and store in a cool, dry, dark, ventilated area. Effective from the date of production, within 6 months. Packaging: 200kg/drum.

THE END